Specifier:  The purpose of this guide specification is to assist the specifier in correctly specifying sheathing products and their installation.  The specifier needs to edit the guide specifications to fit the needs of specific projects.  Contact Huber Engineered Woods to assist in appropriate product selections.  Throughout the guide specification, there are Specifier Notes to assist in the editing of the file. Green text relates to sustainability and red text in brackets indicates a selection needs to be made.

SECTION 06 16 00

SHEATHING & SUBFLOORING

(Huber Engineered Woods – AdvanTech® Wall, Roof, and Floor Sheathing and AdvanTech X-Floor)

      - SECTION INCLUDES

Specifier:  Edit “Section Includes” list to correspond with project specific requirements.

        - Wall sheathing

        - Roof sheathing

        - Subflooring/Underlayment (Floor Sheathing)

      - ACTION SUBMITTALS

        - Product Data:  For each type of sheathing product.  Include manufacturer’s technical data indicating performance properties.

        - Shop Drawings:  Indicating location and extent of sheathing, accessories, and assemblies.  Include details of joints, corners, and penetrations.

      - INFORMATIONAL SUBMITTALS

        - Evaluation Reports:  From ICC-ES, for wood sheathing products.

        - Product Certifications:  From manufacturer, indicating that sheathing products comply with indicated ICC-ES Acceptance Criteria.

Specifier: When project is pursuing a sustainable rating system, retain Sustainable Design Submittal paragraph and edit to correspond to the specific Project requirements.  Modify based on rating system being pursued.

Product Data requirement applies to LEED v4, IgCC, ASHRAE 189.1, and Green Globes

Laboratory Test Reports for composite wood applies to LEED v4

        - Sustainable Design Submittals:

          - Laboratory Test Reports: Indicating compliance with requirement for low emitting materials for composite wood products.

          - Certified Wood Certificates:  Certificates indicating that manufacturer is currently certified by an SFI- or FSC- accredited certification body, and chain-of-custody certificates.

          - Sustainability Attributes Verification:  ICC-ES VAR-1012 Verification of Attributes Environmental Report (AdvanTech® Sheathing), or verification of comparable product acceptable to Architect.

Specifier:  Retain or add specific requirements for projects in indicated jurisdictions or where requirements are used as a standard of care.

        - [Code Compliance recognition by Los Angeles Department of Building and Safety.]

        - [Code Compliance with the California [Building] [Residential] Code]]

        - Warranty:  Sample unexecuted copy of manufacturer’s warranty.

      - CLOSEOUT SUBMITTALS

        - Warranty:  Executed copy of manufacturer’s warranty.

      - QUALITY ASSURANCE

Specifier:  Retain “Manufacturer Qualifications” when pursuing a sustainable rating system requiring chain of custody

        - Manufacturer Qualifications:  Capable of demonstrating that all wood procurement operations are conducted in accordance with procedures and policies of the Sustainable Forestry Initiative (SFI) Program, and the SFI 2022 Standards and Rules.

      - DELIVERY, STORAGE, AND HANDLING

        - Comply with manufacturer's written instructions for protection of sheathing products from weather prior to installation.

      - WARRANTY

Specifier:  Verify current warranty provisions for specified products and assemblies

        - Manufacturer's Warranty:  Manufacturer's standard form in which manufacturer agrees to repair or replace products that demonstrate deterioration or failure under normal use due to manufacturing defects within warranty period specified, when installed according to manufacturer's instructions.

          - Warranty Period for Sheathing Products: Limited Lifetime warranty

- PRODUCTS

      - MANUFACTURER

        - Huber Engineered Woods LLC, Charlotte NC; Phone: (800) 933-9220; Website: www.advantechperforms.com; www.huberwood.com.

      - PERFORMANCE REQUIREMENTS

Specifier:  Retain "Fire-Resistance Ratings" Paragraph when sheathing products are used as part of a fire-resistance-rated assembly and must conform to the requirements.

        - Fire-Resistance Ratings:  Where indicated, provide approved products that are part of fire-resistance-rated assemblies tested in accordance with ASTM E119 - Standard Test Methods for Fire Tests of Building Construction and Materials

        - Provide panels that will not delaminate nor require sanding due to moisture absorption while exposed during construction.

        - Panel Thickness:  Provide thickness needed to meet project requirements and comply with referenced performance category, but not less than thickness indicated.

Specifier:  Retain and edit "Wood Panel Products" Article for all projects.

      - WOOD PANEL PRODUCTS

        - Single Source Limitations:  Provide [wall] [floor] [roof] sheathing by a single manufacturer.

Specifier:  Retain and edit "Certified Wood" Paragraph below as appropriate to Project sustainable design requirements.

        - Certified Wood:  Provide sheathing produced from wood obtained from forests certified by an accredited certification body.

        - Oriented Strand Board:  Comply with the following Product Standards:

          - US Department of Commerce DOC PS 2 - Performance Standard for Wood-Based Structural Panels

            - Panels made with binder containing no added urea formaldehyde, with visible grade stamp and field identification.

          - ICC-ES AC182- Acceptance Criteria for Wood Structural Panel Products

Specifier: AdvanTech® superior design strength:  AdvanTech® roof and wall sheathing can support higher snow and ice design loads than commodity OSB and plywood panels. Strength capacities are outlined in ICC-ES ESR-1785.

        - Code Compliance Standard: Panels to comply with building code. ICC-ES ESR-1785 Evaluation Report for AdvanTech Engineered Panels.  Provide ICC-ESR for comparable product acceptable to Architect.

        - Panel Exposure: No damage from weather exposure for up to 500 days.

        - Fastener Marking:  On top panel surface with pre-spaced fastening symbols for 16-inches and 24-inches on center spacing.

Specifier:  Retain one or more of the three following "Sheathing" Articles based upon Project requirements.

      - WALL SHEATHING

Specifier:  AdvanTech® Sheathing is Structural 1 rated for greater resistance to wind and seismic loads

        - Oriented-Strand-Board Wall Sheathing:  Exposure 1, Structural 1 sheathing.

          - Basis-of-Design Product:  Huber Engineered Woods LLC; AdvanTech® Sheathing.

          - Characteristics

            - Span Rating and Performance Category:  Not less than [32/16, 1/2 Performance Category] [40/20, 5/8 Performance Category]

Specifier: Tongue and groove edge profile is available only on 5/8 Performance Category

            - Edge Profile: [Square edge] [Tongue and groove].

      - ROOF SHEATHING

Specifier:  AdvanTech® Sheathing is Structural 1 rated for greater resistance to wind and seismic loads

        - Oriented-Strand-Board Roof Sheathing:  Exposure 1, Structural 1 sheathing.

          - Basis-of-Design:   Huber Engineered Woods LLC; AdvanTech® Sheathing.

          - Characteristics

            - Span Rating and Performance Category:  Not less than [32/16, 1/2 Performance Category] [40/20, 5/8 Performance Category]

Specifier: Tongue and groove edge profile is available only on 5/8 Performance Category

            - Edge Profile: [Square edge] [Tongue-and-groove].

      - SUBFLOOR-UNDERLAYMENT (FLOOR SHEATHING)

        - Oriented-Strand-Board Combination Subfloor-Underlayment:  Exposure 1 floor panels.

          - Basis-of-Design:  Huber Engineered Woods LLC; AdvanTech® Floor Panels.

          - Characteristics

            - Span Rating and Performance Category:  Not less than [20 oc, 19/32 Performance Category] [24 oc Structural 1, 23/32 Performance Category] [32 oc, 7/8 Performance Category] [48 oc, 1-1/8 Performance Category]

            - Edge Profile:  Tongue-and-groove.

            - Surface Finish:  Fully sanded face.

        - Premium Oriented-Strand-Board Combination Subfloor-Underlayment:  Exposure 1 floor panels.

          - Basis-of-Design:  Huber Engineered Woods LLC; AdvanTech X-Factor Floor Panels.

          - Characteristics

            - Span Rating and Performance Category:  Not less than  [24 oc Structural 1, 23/32 Performance Category] [48 oc, 1-1/8 Performance Category].

            - Edge Profile:  Tongue-and-groove.

            - Surface Finish:  Overlay face.

      - FASTENERS

Specifier: Review local building code requirements for fastener size and spacing. Corrosion Resistant fasteners are recommended for use in coastal environments.

        - Fasteners, General:  Size and type complying with manufacturer's written instructions for Project conditions and requirements of authorities having jurisdiction.

        - Nails, Brads, and Staples:  Conform with ICC-ES AC116 - Acceptance Criteria for Nails and Spikes and ICC-ES AC201 Acceptance Criteria for Staples

        - Power-Driven Fasteners:  ICC-ES ESR-1539 - Power Driven Staples and Nails for Use in Engineered and Non-Engineered Connections or ICC-ES NER-272 - Power Driven Staples and Nails for Use in All Types of Building Construction

        - Wood Screws:  Comply with ASME B18.6.1 - Wood Screws (Inch Series)

Specifier: Retain one of two adhesive subparagraphs below (E or F) as applicable when specifying subfloor adhesive.  When determining compliance with VOC content requirements, be sure to use the correct adhesive classification.  It is a common mistake to include aerosol web-spray adhesive in the general-purpose category.  Aerosol and cartridge adhesives have unique VOC content limitations and therefore it is imperative that the correct classification is referenced.

        - General Purpose Subflooring Panel Adhesive:

          - Characteristics:

            - Polyurethane or solvent-based

            - Panel manufacturer and adhesive manufacturer recommended for indicated use

            - Conforms with ASTM D3498 - Standard Specification for Adhesives for Field-Gluing Structural Panels to Wood Based Floor System Framing [and] [or] APA AFG-01 - Adhesives for Field-Gluing Plywood to Wood Framing.

Specifier: Use maximum VOC content requirements for aerosol web-spray adhesives when using AdvanTech Subfloor Adhesive.

        - Web-Spray Subflooring Panel Adhesive: High performance, moisture-cured, gun-applied polyurethane aerosol web-spray construction adhesive. Formulated to adhere to wet and frozen structural subfloor panels and wood framing.

          - Basis-of-Design:  Huber Engineered Woods AdvanTech™ Subfloor Adhesive

          - Characteristics

            - Polyurethane Aerosol Web-Spray Adhesive

            - Application: Gun applied.

            - VOC 15% by weight (155 g/L).

            - Solids by Weight: 15% maximum.

            - Coverage Rate: 400 linear feet at 3/8” gel bead.

            - Conforms with ASTM D3498 - Standard Specification for Adhesives for Field-Gluing Structural Panels to Wood Based Floor System Framing and APA AFG-01 - Adhesives for Field-Gluing Plywood to Wood Framing.

- EXECUTION

      - EXAMINATION

        - Examine framing spacing and alignment to determine if work is ready to receive sheathing.  Proceed with sheathing work once conditions meet requirements.

      - WOOD STRUCTURAL PANEL INSTALLATION

        - Sheathing Installation, General:  Install sheathing panels in accordance with manufacturer's written instructions, requirements of applicable Evaluation Reports, and requirements of authorities having jurisdiction.

          - Do not bridge expansion joints; allow joint spacing equal to spacing of structural supports.

          - Stagger end joints of adjacent panel runs.

          - Continuously support panel ends.

          - Continuously support panel edges without tongue-and-groove edge profile where indicated.

          - Attach sheathing panels securely to substrate with manufacturer-approved fasteners in compliance with the following:

            - ICC-ES ESR-1539 - Power Driven Staples and Nails for Use in Engineered and Non-Engineered Connections or ICC-ES NER-272 - Power Driven Staples and Nails for Use in All Types of Building Construction Retain one of two subparagraphs based on applicable building code for project.

Specifier: Retain one of two subparagraphs based on applicable building code for project.

            - [ICC IBC - International Building Code Table 2304.9.1 Fastening Schedule.]

            - [ICC IRC - International Residential Code for One- and Two-Family Dwellings: IRC Table R602.3(1), Fastener Schedule for Structural Members, and   R602.3(2), Alternate Attachments.]

          - Comply with applicable portions of The Engineered Wood Association APA  Form No. E30 - Engineered Wood Construction Guide

          - Optimize joint arrangements resulting in minimum number of joints. Cut panels cleanly at penetrations.

        - Combination Subfloor-Underlayment Fastening

- Specifier: Retain the type of framing that sheathing is being attached to – wood or metal.   For wood framing the attachment methods are listed in ascending order of best practice   nail = Good   glue & screw = Best

          - [Wood Framing: [Nail] [Glue and nail] [Screw] [Glue and screw]. Penetrate wood framing members at least 1 inch.]

          - [Cold-Formed Metal Framing:  Glue and screw.]

          - Space panels 1/8 inch apart at supported panel ends.

          - Install fasteners 3/8 inch to 1/2 inch   from panel edges.

          - Space fasteners 6 inches on centers on supported panel ends and 12 inches on centers at intermediate support locations.

Specifier:  Retain subparagraph below if panels in this configuration are required for Project.

            - Space fasteners for 1-1/8 inch  panels supported at 48 inch  spacing 6 inches on centers on supported panel edges and intermediate support locations.

        - [Wall] [and] [Roof] Sheathing Fastening

          - [Wood Framing:  Nail; penetrate wood framing members at least 1 inch.]

          - [Cold-Formed Metal Framing:  Screw]

          - Space panels 1/8 inch apart at [square edges and] ends.

          - Install fasteners 3/8 inch to 1/2 inch from panel edges.

          - Space fasteners 6 inches on centers on supported panel edges and 12 inches on centers at intermediate support locations.

Specifier:  Retain subparagraph below if panels in this configuration are required for Project.

            - Space fasteners for 1-1/8 inch panels supported at 48 inch  spacing 6 inches on centers, on supported panel edges and intermediate support locations.

- END OF SECTION

DISCLAIMER: 

This Specification have been written as an aid to the professionally qualified Specifier and Design Professional. The use of this Guide requires the sole professional judgment and expertise of the qualified Specifier and Design Professional to adapt the information to the specific needs for the Building Owner and the Project, to coordinate with their Construction Document Process, and to meet all the applicable building codes, regulations and laws. HUBER ENGINEERED WOODS EXPRESSLY DISCLAIMS ANY WARRANTY, EXPRESSED OR IMPLIED, INCLUDING THE WARRANTY OF MERCHANTABILITY OR FITNESS FOR PARTICULAR PURPOSE OF THIS PRODUCT FOR THE PROJECT.