Specifier:  The purpose of this guide specification is to assist the specifier in correctly specifying sheathing products with an integral air and moisture barrier and their installation.  The specifier needs to edit the guide specifications to fit the needs of specific projects.  Contact Huber Engineered Woods to assist in appropriate product selections.  Throughout the guide specification, there are Specifier Notes to assist in the editing of the file. Green text relates to sustainability and red text in brackets indicates a selection needs to be made.

SECTION 06 16 53.01

AIR AND MOISTURE RESISTANT SHEATHING

(Huber Engineered Woods - ZIP System® – Roof and Wall Sheathing)

- GENERAL

      - SECTION INCLUDES

Specifier:  When using ZIP System® sheathing, coordinate/delete air barrier/weather barrier specifications from Division 07 and Sheathing from Division 06.

        - Wall sheathing with integral weather-resistive barrier

        - Roof sheathing with integral roof underlayment.

      - ACTION SUBMITTALS

        - Product Data:  Product Data:  For each type of sheathing product.  Include manufacturer’s technical data indicating performance properties

        - Shop Drawings:  Indicating location and extent of sheathing, accessories, and assemblies.  Include details of joints, corners, and penetrations.

      - INFORMATIONAL SUBMITTALS

        - Evaluation Reports:  From ICC-ES, for wood sheathing and seam tape and flashing.

        - Product Certifications:  From manufacturer, indicating that sheathing products comply with indicated ICC-ES Acceptance Criteria.

Specifier: When project is pursuing a sustainable rating system, retain Sustainable Design Submittal paragraph and edit to correspond to the specific Project requirements.  Modify based on rating system being pursued.

- Product Data requirement applies to LEED v4, IgCC, ASHRAE 189.1, and Green Globes

- Laboratory Test Reports for composite wood applies  to LEED v4

        - Sustainable Design Submittals:

          - Product Data: For liquid applied flashing, indicating VOC content

          - Laboratory Test Reports: Indicating compliance with requirement for low emitting materials for the following:

            - Composite wood products

            - Liquid flashing

          - Certified Wood Certificates:  Certificates indicating that manufacturer is currently certified by an SFI- or FSC- accredited certification body, and chain-of-custody certificates indicating that sheathing products comply with forest certification requirements.

Specifier:  Retain "Florida Building Code Certificate" for Florida projects or where FBC qualification is used as a standard for high wind design areas.

        - Documentation indicating that products comply with requirements of [Florida Building Code] [Florida Residential Code]

        - Warranty:  Sample unexecuted copy of manufacturer warranty.

      - CLOSEOUT SUBMITTALS

        - Warranty:  Executed copy of manufacturer warranty

      - QUALITY ASSURANCE

Specifier:  Retain when pursuing a sustainable rating system requiring chain of custody

        - Manufacturer Qualifications:  Capable of demonstrating that all wood procurement operations are conducted in accordance with procedures and policies of the Sustainable Forestry Initiative (SFI) Program, and the 2015-2019 Standards.

        - [Wall sheathing meeting requirements for water-resistive barrier in accordance with ICC-ES AC310 – Water-resistive Membranes Factory-bonded to Wood-based Structural Sheathing, Used as Water-resistive Barriers.]

        - [Roof sheathing meeting requirements for roof underlayment in accordance with ICC-ES AC266- Wood Structural Panel Roof Sheathing Factory-laminated with an Alternative Roof Underlayment.]

Specifier:  Retain "Florida State Building Code Certificate" for Florida projects or where FSBC qualification is used as a standard. The Florida Product Approval numbers indicated are specific to ZIP System® sheathing, refer to manufacturer literature to confirm current approvals.

        - [Florida Building Code Compliance:  Provide sheathing complying with Florida Building Code product and installation requirements for locations outside of high velocity wind zone.]

          - [Florida Product Approval No. 17146.2 – ZIP System® Roof Sheathing (combination roof sheathing and roof underlayment)]

      - DELIVERY, STORAGE, AND HANDLING

        - Comply with manufacturer's written instructions for protection of sheathing products from weather prior to installation.

      - WARRANTY

Specifier:  Verify warranty provisions for specified products.  Huber Engineered Woods LLC offers warranty periods of up to 30 years for ZIP System® sheathing.

        - Manufacturer's Warranty:  Manufacturer's standard form in which sheathing manufacturer agrees to repair or replace sheathing products that demonstrate deterioration or failure under normal use due to manufacturing defects within warranty period specified, when installed according to manufacturer's instructions.

          - Warranty Period for Sheathing Products: [30] years from date of Substantial Completion.

- PRODUCTS

      - MANUFACTURER

        - Huber Engineered Woods LLC, Charlotte NC; Phone: (800) 933-9220; Website: www.huberwood.com

      - PERFORMANCE REQUIREMENTS

Specifier:  Retain appropriate "Fire-Test-Response" Paragraph when sheathing products are used as part of a fire-resistance-rated assembly and must conform to the requirements.

        - Fire-Test-Response Characteristics:

          - Fire-Resistance Ratings (Wall sheathing):  Where indicated, provide approved products that are part of fire-resistance-rated assemblies tested in accordance with  ASTM E119 - Standard Test Methods for Fire Tests of Building Construction and Materials

          - Exterior Fire-Test Exposure (Roof sheathing):  Where indicated provide approved products that are part of fire-resistance-rated assemblies with approved Class A coverings, tested in accordance with ASTM E108 – Standard Test Methods for Fire Test of Roof Coverings

        - Air-Barrier Assembly Air Leakage:  Less than 0.04 cfm/sq. ft. at 1.57 lbf/sq. ft. (0.2 L/s x sq. m at 75 Pa), per ASTM E2357 – Standard Test Method for Determining Air Leakage of Air Barrier Assemblies

        - Water-Vapor Permeance, Facer:  Minimum 12 perms (689 ng/Pa x s x sq. m),  when tested in accordance with ASTM E96/E96M – Standard Test Methods for Water Vapor Transmission of Materials.

Specifier:  Retain and edit "Wood Panel Products" Article for all projects.

      - WOOD PANEL PRODUCTS

        - Single Source Limitations:  Provide [Wall sheathing with integral weather-resistive barrier] [and] [roof sheathing with integral roof underlayment] by a single manufacturer.

Specifier:  Retain and edit "Certified Wood" Paragraph below as appropriate to Project sustainable design requirements.

        - Certified Wood:  Provide sheathing produced from wood obtained from forests certified by an accredited certification body.

        - Oriented Strand Board:  US Department of Commerce DOC PS 2 - Performance Standard for Wood-Based Structural Panels

          - Panels made with binder containing no added urea formaldehyde.

        - Panel Exposure: No damage from weather exposure for up to 180 days.

        - Printed fastener spacing symbols on facer for 16-inch (406 mm) and 24-inch (610 mm) on center spacing.

      - WALL SHEATHING WITH INTEGRAL WEATHER-RESISTIVE BARRIER

Specifier:  Huber's ZIP System® sheathing may be used as wall sheathing on buildings of Type V construction and construction permitted under the IRC with allowable code-compliant exterior wall coverings.  When ZIP System® wall sheathing is required, moisture barriers such as building paper or housewrap are not required. In wall covering systems requiring multiple layers of water-resistive barriers, ZIP System® sheathing is intended to replace only the first layer.

ZIP System® roof and wall sheathing provide Exposure 1, Structural 1 and have an integral water-resistive barrier and air barrier.    Check with your local Huber Engineered Woods representative or call 1-800-933-9220 ext. 5022 for availability.

        - Oriented-Strand-Board Wall Sheathing:  Exposure 1, Structural 1 sheathing with factory-laminated water-resistive barrier facer and printed fastener location symbols.

          - Basis-of-Design:  Huber Engineered Woods LLC; ZIP System® sheathing.

          - Characteristics

            - Span Rating and Performance Category:  Not less than [24/16; Structural 1; 7/16 Performance Category] [32/16; Structural 1; 1/2 Performance Category] [40/20; Structural 1; 5/8 Performance Category].

            - Edge Profile:  Tongue-and-Tongue along long edges and square-edge along 4 ft edges.

            - Weather Barrier Facer:  Medium-density, phenolic-impregnated sheet material qualifying as an ASTM D779 Grade D weather-resistive barrier in accordance with ICC-ES AC38 – Water-Resistive Barriers

      - ROOF SHEATHING WITH INTEGRAL ROOF UNDERLAYMENT

Specifier: Huber's ZIP System® sheathing may be used as roof sheathing on buildings of Type III or V construction and construction permitted under the IRC with allowable non-classified roof coverings using code-complying asphalt-fiberglass shingles, metal shingles, metal panels, wood shakes, wood shingles, slate shingles or slate-like composite shingles, and clay and concrete tile roof coverings. Installation is limited to roofs having slopes of 2:12 (16.67 percent) or greater.  Felt underlayment is not required on the roof.  In roof covering systems requiring multiple layers of roofing underlayment, ZIP System® sheathing is intended to replace only the first layer.

        - Oriented-Strand-Board Roof Sheathing:  Exposure 1 sheathing with factory-laminated water-resistive barrier facer with printed fastener location symbols.

          - Basis-of-Design:  Huber Engineered Woods LLC; ZIP System® sheathing.

          - Characteristics

            - Span Rating, Panel Grade and Performance Category:  Not less than [24/16; Structural 1; 7/16 Performance Category] [32/16; Structural 1; 1/2 Performance category] [40/20; Structural 1; 5/8 Performance Category].

Specifier:  Tongue-and-Groove edge profile is only available in 5/8 Performance Category ZIP System® sheathing. It may also have limited availability by region.  Contact Huber Engineered Wood for additional information.

            - Edge Profile: [Tongue-and-Tongue] [Tongue-and-groove] and square-edge along 4 ft edges.

            - Exterior Surface Facer:  Medium-density, phenolic-impregnated kraft paper overlay in accordance with ICC-ES AC266 – Wood Structural Panel Roof Sheathing Factory-laminated with an Alternative Roof Underlayment.

Specifier:  7/16 Performance Category ZIP System® sheathing requires edge support (Approved H-Clips or blocking) when installed on roof supports spaced greater than 16-inches.  Approved Panel edge clips are Simpson Strong-Tie® PSCA7/16, PSCL7/16 and TAMLYN PCS7/16.

        - Panel Edge Clips:  Provide panel edge clips approved for roof application in accordance with code approvals and panel manufacturer's written instructions.

      - FASTENERS

Specifier: Review local building code requirements for fastener size and spacing. Corrosion Resistant fasteners are recommended for use in coastal environments.

        - Fasteners, General:  Size and type complying with manufacturer's written instructions for Project conditions and requirements of authorities having jurisdiction.

          - [Corrosion Resistant]

        - Nails, Brads, and Staples:  Conform with ICC-ES AC116 - Acceptance Criteria for Nails and Spikes and ICC-ES AC201 Acceptance Criteria for Staples

        - Power-Driven Fasteners:  ICC-ES ESR-1539 - Power Driven Staples and Nails for Use in Engineered and Non-Engineered Connections or ICC-ES NER-272 - Power Driven Staples and Nails for Use in All Types of Building Construction

      - ACCESSORY PRODUCTS

Specifier: Huber's ZIP System™ tape is used to tape sheathing panel joints and may also be used as flexible flashing around window frames, door frames, wall penetrations, and transitions to other materials.

        - Self-Adhering Seam and Flashing Tape:  Pressure-sensitive, self-adhering, cold-applied, seam tape consisting of polyolefin film with acrylic adhesive, meeting ICC-ES AC148 – Acceptance Criteria for Flexible Flashing Materials, and tested as part of an assembly meeting performance requirements.

          - Basis-of-Design:  Huber Engineered Woods; ZIP System™ flashing tape.

          - Characteristics

            - Adhesive type:  Acrylic

            - Thickness:    0.012 inch (0.3 mm).

            - Tensile Strength:  938 psi

            - Elongation:  400-800 percent

            - Complies with AAMA 711 – Voluntary Specification for Self Adhering Flashing Used for Installation of Exterior Wall Fenestration and ICC-ES AC148 – Acceptance Criteria for Flexible Flashing Materials,

Specifier: Huber's ZIP System™ liquid flash works in conjunction with or in place of ZIP System™ tape to permanently flash and seal building penetrations and panel seams.

        - Liquid-Applied Flashing Membrane: Gun-grade, cold-applied, silyl-terminated polymer (STP) liquid flashing membrane compatible with sheathing/weather barrier, self-adhering seam and flashing tape, and tested as part of an assembly meeting performance requirements.

          - Basis-of-Design:  Huber Engineered Woods; ZIP System™ Liquid Flash.

          - Characteristics

            - Composition:  Single component silyl-terminated polymer (STP)

            - Application Temperature Range: Between 35 Deg F (2 Deg C) and 110 Deg F (43 Deg C) surface and ambient.

            - VOC Content:  30 g/L

            - Hardness, Shore A:  40 to 45 in accordance with ASTM C661 – Standard Test Method for Indentation Hardness of Elastomeric Type Sealants by Means of a Durometer

            - Tensile Strength:  75 psi in accordance with ASTM D412 – Standard Test Methods for Vulcanized Rubber and Thermoplastic Elastomers

            - Elongation at Break:  225 percent in accordance with ASTM D412 – Standard Test Methods for Vulcanized Rubber and Thermoplastic Elastomers

Specifier: Huber's ZIP System™ stretch tape may be used as flexible flashing around windows and window frames, door frames, and wall penetrations. ZIP System™ stretch tape is an innovative construction tape that stretches and forms around irregular and difficult to seal areas.  It is resistant to UV exposure for up to 180-days and has a 30-year limited system warranty when used with ZIP System® sheathing.

        - Self-Adhering Flexible Flashing Tape:  Pressure-sensitive, self-adhering, cold-applied, seam tape consisting of polyolefin film with acrylic adhesive; tested as part of an assembly meeting performance requirements.

          - Basis-of-Design:  Huber Engineered Woods; ZIP System™ stretch tape.

          - Characteristics

            - Adhesive type:  Acrylic

            - Thickness:  0.042 inch (1.067 mm).

            - Tensile Strength:  225 psi

            - Elongation:  800-1200 percent

            - Complies with AAMA 711 – Voluntary Specification for Self Adhering Flashing Used for Installation of Exterior Wall Fenestration and ICC-ES AC148 – Acceptance Criteria for Flexible Flashing Materials

- EXECUTION

      - EXAMINATION

        - Examine framing spacing and alignment to determine if work is ready to receive sheathing.  Proceed with sheathing work once conditions meet requirements.

      - SHEATHING INSTALLATION

        - General:  Install sheathing panels in accordance with manufacturer's written instructions, requirements of applicable Evaluation Reports, and requirements of authorities having jurisdiction.

          - Do not bridge expansion joints; allow joint spacing equal to spacing of structural supports.

          - Install panels with laminated facer to exterior.  Stagger end joints of adjacent panel runs.  Support all panel edges.

          - Panel Edge Spacing:  In accordance with sheathing panel manufacturer’s recommendations.

          - Attach sheathing panels securely to substrate with manufacturer-approved fasteners in compliance with the following:

            - ICC-ES ESR-1539 - Power Driven Staples and Nails for Use in Engineered and Non-Engineered Connections or ICC-ES NER-272 - Power Driven Staples and Nails for Use in All Types of Building Construction

Specifier:  Retain one of two subparagraphs based on applicable building code for project.

            - [ICC IBC - International Building Code Table 2304.9.1 Fastening Schedule.]

            - [ICC IRC - International Residential Code for One- and Two-Family Dwellings: IRC Table R602.3(1), Fastener Schedule for Structural Members, and   R602.3(2), Alternate Attachments.]

Specifier:  7/16 Performance Category ZIP System® sheathing requires edge support (Approved H-Clips or blocking) when installed on roof supports spaced greater than 16-inches on-center. Approved panel edge clips include Simpson Strong-Tie® PSCA7/16, PSCL7/16 and TAMLYN PCS7/16.

          - [Install Roof Sheathing Panel Clips where required under code approvals based upon panel thickness and support spacing, provide panel clips located at each unsupported panel butt joint centered between supports.]

      - SEAM AND PENETRATION TREATMENT

        - Assembly continuity:  Coordinate sheathing installation with flashing and joint sealant sequencing and installation and with adjacent building air and moisture barrier components to provide complete, continuous air- and moisture- barrier.

        - Tape panel seams, penetrations, and facer defects or cracks with self-adhering seam tape [ZIP System™ Flashing Tape] to form continuous weathertight surface.  Apply tape according to manufacturer's written instructions and requirements of ICC-ES applicable to tape application.

        - Flash penetrations, gaps, and cracks with liquid-applied flashing membrane [ZIP System™ Liquid Flash] to form continuous weathertight surface. Apply according to manufacturer's written instructions.  Follow manufacturer’s recommendation for integration with self-adhering seam tape [ZIP System™ Flashing Tape].

        - Tape window and doors openings and radius penetrations with self-adhering flexible flashing tape [ZIP System™ Stretch Tape] to form continuous weathertight surface. Apply tape according to manufacturer’s written instructions and requirements of ICC-AC applicable to tape application.

END OF SECTION

DISCLAIMER: 

This Specification have been written as an aid to the professionally qualified Specifier and Design Professional. The use of this Guide requires the sole professional judgment and expertise of the qualified Specifier and Design Professional to adapt the information to the specific needs for the Building Owner and the Project, to coordinate with their Construction Document Process, and to meet all the applicable building codes, regulations and laws. HUBER ENGINEERED WOODS EXPRESSLY DISCLAIMS ANY WARRANTY, EXPRESSED OR IMPLIED, INCLUDING THE WARRANTY OF MERCHANTABILITY OR FITNESS FOR PARTICULAR PURPOSE OF THIS PRODUCT FOR THE PROJECT.